MANGALORE REFINERY AND PETROCHEMICALS LIMITED (MRPL)
TECHNICAL SERVICES & PLANT INTEGRITY DIVISION • CONFIDENTIAL INTERNAL USE ONLY

# CDU-II Atmospheric Column C-101 Overhead Vapor Line Asset Integrity Assessment

| Refinery Operating Unit: | CDU-II (Atmospheric Distillation Complex) |
| --- | --- |
| Governing SOP Standard: | SOP-MRPL-4.2.3 |
| Lead Inspection Engineer: | Akshitha Rachakonda (Sr. Integrity Engineer) |

## 1. Inspection Observations & Evidence Matrix

The following findings were extracted directly from the primary inspection report and cross-verified against MRPL maintenance standards. Each finding maintains cryptographic provenance to its source document.

| Finding | Source Page & Region | Technical Observation | SOP Match | Confidence |
| --- | --- | --- | --- | --- |
| #1 | Scanned Inspection Report, Page 6 (Tray 44 Nozzle) | Localized naphthenic acid thinning; wall thickness 6.1 mm (min standard 6.5 mm) | SOP-MRPL-4.2.3 | 94% |
| #2 | Scanned Inspection Report, Page 9 (Condenser Boot Flange) | Greenish-white salt weeping indicating ammonium chloride deposition | SOP-MRPL-4.2.3 | 91% |

## 2. Engineering Recommendations & Corrective Plan

Flag Tray 44 overhead nozzle as Category-A Defect. Recalibrate neutralizing amine injection rate to hold overhead boot water pH strictly between 5.8 and 6.8. Fabricate and install a bypass spool for the Tray 44 nozzle and schedule nozzle replacement during the next CDU-II turnaround. Conduct a full-column overhead nozzle ultrasonic thickness survey to map the extent of naphthenic-acid / ammonium-chloride corrosion before any derating decision.

## 3. Regulatory & Human Review Sign-Off

Prepared by: _________________________		Approved by: _________________________
Lead Plant Engineer (Operations)		Chief General Manager (Refinery)